## Slide 1: X-Ray standing waves for investigation of periodic multilayers.
DESY Summer Student Program 2012
Elena Pavlenko
Moscow State University, Russia.
DESY September 06, 2012
Notes: Hello my name is Elenea pavlenko and my presentation is about X-Ray standing waves for investigation of periodic multilayers.

## Slide 2: Contents
Introduction to:
  Multilayers
  X-ray standing waves
  Fluorescent yields
Modeling process
Results and analysis
Conclusion
Notes: I will start with a bit of the background behind my experiment including an introduction to multilayer ,X-ray standing waves and fluorescence yields. I will then discuss the modeling process. Finally I will talk about my results.

## Slide 3: Multilayers: what for ?
Industry
Free electron lasers
Lithography
Extreme ultraviolet radiation
~ 10nm=100Å
Multilayer system, with 100Å depth period.
Notes: Extreme ultraviolet light is used in many areas of science and different industry sectors.
To manipulate this light, you needed structures which have a interplanar distance similar to the wavelength of the light,
which is about hundreds of Angstroms.
In typical crystal the distance between layers of atoms is too small - it is about several angstroms and that's why these crystals are unsuitable
Multilayer – it is a structure which consist of two repeating layers with different density.

## Slide 4: Multilayers: method of investigation
~ 1000nm=100Å
Multilayer system, with 100Å depth period.
Method of investigation
X-Ray Standing Waves
Notes: for use these multilayers, they must be of good quality. To study the quality of the multilayer we use Xray standing waves. For any standing wave phenomena, the minimum requirement is the superposition of two coherently plane waves. In the multilayer, the interference between the incident and reflected waves satisfies these conditions producing an X-ray standing wave above the reflecting interface.

## Slide 5: Aims
Apply the method of X-ray standing waves to investigate a B/Mo multilayer crystal
Parameterize a model to describe the multilayers:
  Fluorescence yield
  Reflectivity
  Electric Fields
Notes: Here is the aims of the project
The first aim is to study the quality the of a Boron Molybdenum multilayer crystal using the X ray standing wave method. Then we wish to create and parameterize a model which describes the electric fields, reflectivity and fluorescence yield of the multilayer.

## Slide 6: Multilayer object layout
B (20Å)
Si
Mo(14Å)
B(20Å)
B(20Å)
La(3Å)
50 layer pair
Mo(14Å)
B (20Å)
It is assumed that the multilayer is of high quality and all B/Mo double layer pairs are equivalent
Top layers
Notes: Each period of the multilayer structure consist of a layer of Boron and a layer of molybdenum. This period is repeated 50 times in the structure and on the top we have three layers which help us to investigate the quality of the multilayer by fluorescence yield. If the structure is of good quality then we can assume that each double layer pair is equivalent.

## Slide 7: X-ray standing waves from periodic multilayers
Electromagnetic field distribution inside a multilayer in depth and in angle.
Fluorescence yield from atoms at different depths
Notes: We modeled the electric field that is formed by the standing waves in the multilayer structure assuming the layers are equivalent. The left images shows how the electric field changes as a function of the angle of incidence and depth in the multilayer. The standing wave’s electric field creates secondary process in the crystal. Electromagnetic feald gives energy to atoms of substance and than they begin emit energy by themselves. This cold secondary process. one such secondary process is fluorescence. Secondary process are proportional to the intensity of the electric field. The second graph shows the angular dependence of the fluorescence yield for several different depths.

## Slide 8: Experiment & data evaluation : X-ray reflectivity measurements
- goodness of fit.
Fit of the reflectivity curve.
Notes: The reflectivity curves from the layers contain a series of diffraction peaks and the interference oscillations between them. To obtain the information about the structure, the standard procedure of fitting theoretical curves to the experimental data was used. The degree of convergence of the experimental data with the theoretical model is evaluated using the parameter 2 The 2 value is given by the following equation: Where n is the number of data points, Np is the number of unknown parameters, Iexp and Icalc are the measured and calculated theoretical intensity and sj is the statistical error. A low chi squared indicates a good fit, so this fit is quite good.

## Slide 9: Experiment & data evaluation: X-ray standing waves
Fit of the fluorescence yield.
Notes: Electromagnetic field in the sample was calculated using the model of the sample obtained from the previous fit. The theoretical curve of the fluorescence yield is calculated from the field pattern. Plotted on the graph is the fluorescence yield from the experimental data (blue points) and from the model (black line). It can be seen that the curve calculated theoretically does not accurately describe the oscillations in the tail of the curve. In this case, the convergence of theory and experiment is not satisfactory. This fact indicates that the calculated model is not that accurate.

## Slide 10: Data evaluation: problems
Fit of the reflectivity curve.
The assumption of the equivalence of the layers was not really correct. Every layer should be considered independently.
Notes: On the curve of reflectivity this disagreement may affect the oscillations, which are situated between the Bragg peaks. Indeed, if you look at the details of reflectivity curve fit, you can see disagreement between theory and experiment in thas area of the curve. Thus we can conclude that our assumption that the multilayer periods were equivalent is not correct. Instead we should consider the layers independently.

## Slide 11
Data evaluation: X-ray reflectivity, better fit
Fit of the reflectivity curve with treating the layers independently.
Notes: This is results of the second fit where we have treated each layer independently. Now the parameter 2 is even less, giving more evidence that agreement between theory and experiment is much better

## Slide 12: Data evaluation: X-ray reflectivity, better fit
Fit of the reflectivity curve.
Notes: If we again have a closer look at the reflectivity curve we can see that the agreement is much better than before. Now the oscillations in the data set is well described by our fit.

## Slide 13: X-ray standing waves, final result
Fit of the fluorescence yield.
Notes: Looking at our updated fluorescence yield graph we see that the new fit describes the oscillations in the tails much more accurately.
There is still room for improvement in our model as it does not yet completely describe the tail oscillations.

## Slide 14: Conclusions
1) X-ray standing wave method has been used for the analysis of periodic multilayers.
2) The model structure proposed by deposition team has been checked.
3) The model which correctly describes the investigated multilayer structure was created.
4) The lack of equivalence of each layer implies the crystal is not of great quality.
Notes: X-ray standing wave method has been implemented for the analysis of periodic multilayers. The model structure proposed by deposition team has been checked. The model which correctly describes the investigated multilayer structure was created. This model is based on the analysis of the measured data. It is shown that the method of X-ray standing waves delivers complimentary information on multilayer structure. The lack of equivalence of each layer implies the crystal is not of great quality

## Slide 15: Acknowledgements
Kurchatov institute
Desy Summer student program
Supervisors
Dmitryi Novikov
Sergey Yakunin
Notes: I would quickly like to thank the Kurchatov institute for supply the software used in my analysis. I would also like to thank everyone involved in running the DESY summer student program for a fantastic 7 weeks in which I have learnt a huge amount. In particular I would like to thank …….. And …………………… for all their support and all the knowledge they have given me. Thanks.

## Slide 16: Thank you for your attention!
Thank you for your attention!